TECHNICAL SPECIFICATIONS

MELAMINE MOULDING COMPOUND

# *PROPERTIES OF MOULDING POWDER

(1) Appearance			Sprea			Translucent to opaque

(2) Colours		   	   “			Unlimited

(3) Moulding quality	   	   “			Excellent

(4) Type of material	   	   “			Thermosetting

(5) Moulding temperature	   “			135-177 C

(6) Bulk density			DIN 53468		600/650 gm/l

(7) Flow			DIN 53465		170/230 mm x 10

*SPECIFICATIONS OF MELAMINE MOULDING COMPOUND

Exp.			Test			Value		Unit

(1) Specific Weight		DIN 53479		1.5		gm/cm3

(2) Impact strength		DIN 51453		6.5		kJ/m2

(3) Notch impact strength	DIN 51453		1.5		kJ/m2

(4) Bending strength		DIN 51230		800		kP/cm2

(5) Compression strength	DIN 53454		2000		kP/cm2

(6) Tensile strength		DIN 53455		300		kP/cm2

(7) Stability under heat		DIN 53458		100		C

(8) Tracking resistance		DIN 53480		3

(9) Dielectric rigidity		DIN 53483		12		kV/mm

(10) Electric strength		DIN 53481		8-15		kV/cm

(11) Ignition			DIN 53459		3

(12) Shrinkage			DIN 53464		0.9		%

(13) Surface resistance		DIN 53482		Good

(14) Particle size		DIN 53477

(15) Cold water absorption	DIN 7708	sheet 2  150		mg

(16) Hot water absorption	DIN 7708	sheet 3  200		mg

(17) Flexural strength		DIN 53452		80		N/mm2

*PROPERTIES OF STORAGE

- Storage at 25 C gives stability for 6 months. A higher temperature affects the materials flow and its mouldability.

- Melamine Moulding Compound is packed in 25 kg strong export bags unitized on non-returnable wooden pallets.