VENEER TAPES AND GLUE THREADS

I	Green Veneer Tape/Reeling Tape/Non-Perforated Tape

No.		Item			Size					Qty/Box

1.		Reeling Tape		09mm x 550m (3/8inch x 1800ft)	40 rolls

2.		Reeling Tape		09mm x 1000m (3/8inch x 3300ft)	30 rolls

3. 		Reeling Tape		13mm x 550m (1/2inch x 1800ft)	30 rolls

4.		Reeling Tape		13mm x 1000m (1/2inch x 3300ft)	20 rolls

II	Dry Veneer Tape/Gummed Tape/Perforated Tape

#### No.		Item			Size					Qty/Box

1.		Gummed Tape	16mm x 300m (5/8inch x 1000ft)	40 rolls

2.		Gummed Tape	16mm x 550m (5/8inch x 1800ft)	30 rolls

3.		Gummed Tape	16mm x 1000m (5/8inch x 3300ft)	10 rolls

4.		Gummed Tape	19mm x 300m (3/4inch x 1000ft)	40 rolls

5.		Gummed Tape	19mm x 550m (3/4inch x 1800ft)	20 rolls

6.		Gummed Tape	19mm x 1000m (3/4inch x 3300ft)	10 rolls

7.		Gummed Tape	25mm x 300m (1 inch x 1000ft)	40 rolls

8.		Gummed Tape	25mm x 550m (1 inch x 1800ft)	20 rolls

III 	Glue Threads for Sliced and Rotary Cut Veneer

CS 01-D  – Recommended for sliced veneer from 0.5 to 0.8 mm

CS 02-D  – Recommended for rotary cut veneer from 1.0 to 5.0 mm

- Impregnated with polyamide based resin

- Torsion of fiber glass thread Class E – Torsion Z

- Resin softening point is 130 - 140 C

- Average weight of one full spool is 1600-1650 g. Empty spool weighs 160 g.

- Average length per spool is 12000-12600 linear meters (CS 01-D) and 7700-8200 linear meters (CS 02-D)

- Specific weights are 120 g +/- 10 g per 1000 m (CS 01-D) and 160 g +/- 10 g per 1000 m (CS 02-D)

- CS 10-D: Small bobbins of 144 g +/- 5% by 1200 linear meters. Ideal for small manual repairs of veneers.

- Packaging in boxes containing 8 spools (CS 01 and CS 02) and 20 or 80 small bobbins of CS 10-D.

- Spools are compatible with Kuper and other jointing machines.

- Release agent available.

#### IV Polyester Compound Glue threads for Composers

##### Characteristics and Application

Detex 1100 Thread is made of 100% fiber compound polyester (without torsion).

When glue-impregnated with hot melt adhesive it is applied on stringing wooden strips for block board and veneer jointers (composers), e.g. Benecke, Miname, Meinan and others. Supplied normally in spools of 3 kg = 24 000 linear meters (1 linear meter = 0.136 g).

Detex 1670 Thread is normally used for thick veneers and block board. Supplied normally in spools of 3 kg = 18 000 linear meters (1 linear meter = 0.168 g).

##### Technical Specifications

Nominal linear density              	1100 Decitex

Typical linear density                 	1120 Decitex

Number of filaments                             192 units

Force resistance (rupture)		82,0 Newton

Tenacity                                              73,2 cN/tex

E.A.S.L.		                   	13,2 %

Continuous thread (no knots)      	yes

Torsion                                                no tpm

Oil-content                                           0,65 %

Active adhesive                                    none

CALL US FOR MORE INFORMATION AND PRICE QUOTES!