TECHNICAL SPECIFICATIONS

MELAMINE CRYSTAL POWDER

# TECHNICAL DATA

Appearance:  		White Crystal Powder, lnnocuous, Sans Taste.

Density: 		1570 kg/m3

Stacking Density:	700-900 kg/m3

Melting Point: 		at 354 Centigrades decompose and sublimate under ambient pressure

Specific Heat:		1.473Kj/Kg/Centigrade

Specifications:
Purity:			99.8%	Min.
Moisture:			0.1%	Max.
Ash:			0.035	Max.
Color	(APHA):	20	Max.
Hazen:			20	Max.
pH:			7.5-9.5
Appearance: 		White powder without foreign substance

##### Packing: 	in 25kg, 500kg, 1000kg net PP woven bag with PE liner bag