TECHNICAL SPECIFICATIONS

PARAFORMALDEHYDE

UN 2213		IMCO 4.1

Mol. Formula 	[-CH2O-]n  n = 8x100 as the mix of Polyoxymethylene Glycols

Application		Used in production of synthetic rubbers, glues, pharmaceuticals and agricultural chemicals

| Appearance Melting point, °C max. Mass fraction of Formaldehyde, % Mass fraction of Ash, % max. Solution in water, % Residue on the mesh No. 4 | White powder / prills 145 94-98 0.05 Close to 100 Absent |
| --- | --- |

Packing in 25 kg 6-ply paper bags with inner PE.

Loading capacity	17.8 MT net per 20` FCL