TECHNICAL SPECIFICATIONS

PHENOLIC MOULDING COMPOUND

BLACK “GE 31”

# *PROPERTIES OF MOULDING POWDER

(1) Appearance			Sprea			Opaque colours

(2) Colours		   	   “			Black

(3) Moulding quality	   	   “			Excellent

(4) Type of resin	   	   “			Thermosetting

(5) Moulding temperature	   “			155 - 165 C

(6) Bulk density			DIN 53468		570 - 590 gm/l

(7) Flow			DIN 53465		45 - 55

*SPECIFICATIONS OF PHENOLIC MOULDING COMPOUND

Exp.			Test			Value		Unit

(1) Specific Weight		DIN 53479		1.3		gm/cm3

(2) Impact strength		DIN 51453		6.5		kJ/m2

(3) Notch impact strength	DIN 51453		1.5		kJ/m2

(4) Bending strength		DIN 51230		800		kP/cm2

(5) Stability under heat		DIN 53458		120		C

(6) Dielectric rigidity		DIN 53483		12		kV/mm

(7) Electric strength		DIN 53481		8-15		kV/cm

(8) Ignition			DIN 53459		3		-

(9) Shrinkage			DIN 53464		0.9		%

(10) Surface resistance		DIN 53482		Good		-

(11) Particle size		DIN 53477		Upon request	-

(12) Cold water absorption	DIN 7708	sheet 2  150		mg

(13) Hot water absorption	DIN 7708	sheet 3  200		mg

*PROPERTIES OF STORAGE

- Storage at 25 C gives stability for several years. A higher temperature affects the material flow and mouldability.

- Phenolic Moulding Compound is packed in 25 kg strong export bags unitized on non-returnable wooden pallets.