STRONGBOND 888
(For Parquet Flooring)

SB-888 is a specially developed Spray dried Resin Powder used for 3-layer parquet production. The Glue derived out of this resin powder in combination with Enhancer, Modifier and Hardener, will have the following advantages. - Low Formaldehyde Emission. - Higher Bonding Strength. - Glue formulation is flexible to the pressing condition. - Prevents panel warping.

PHYSICAL PROPERTIES

| Appearance | : | White Free Flowing Powder |  |
| --- | --- | --- | --- |
| Viscosity (2:1 soln.at 25 deg.C ) | : | 3500-4500 cps. |  |
| Shelf Life | : | 6 months at 30 deg.C |  |
| Packing |  | 25 Kgs in PP Bags |  |

GLUE FORMULATION

Part A

| Powder Resin |  | 100 Kgs. |  |
| --- | --- | --- | --- |
| Water |  | 50-60 Kgs. |  |
| Enhancer |  | 25-30 Kgs. |  |
| Modifier |  | 5-10 Kgs. |  |

Part B

| Hardner |  | 100 Kgs. |  |
| --- | --- | --- | --- |
| Water |  | 75-85 Kgs. |  |

Final Mix

| Part A |  | 100 |  |
| --- | --- | --- | --- |
| Part B |  | 10-15 |  |

MIXING PROCEDURE

Making of Part A

- First take water in the mixer.

- Add Enhancer and mix well.

- Add Resin Powder and mix well till homogeneous mixing is achieved.

- Add modifier and mix thoroughly.

Making of Part B

- In another Mixer take water and Hardener and mix well.

- Finally Mix Part A and Part B as per the above ratio and the glue is ready for use.

PRESSING PARAMETERS

| Veneer |  | Moisture content of the veneer should be 8-12%. |
| --- | --- | --- |
| Glue Spreading |  | About 200 +/-20 gm/m2. Spread depends in the surface quality. |
| Pressure |  | 10-15 kg/cm2 |
| Pressing Time |  | depends on the amount of hardener, veneer thickness, moisture content, platen temperature, etc. |

Following parameters may be recommended for parquet production, for a 4 mm thickness face veneer.

| Press Temp./deg.C | Pass Time /minsB |
| --- | --- |
| 80 | 10-12 |
| 90 | 8-10 |
| 100 | 5-7 |
| 110 | 3-5 |

NOTE Information on this page is based on the best of our knowledge. However, since conditions under which our products may be used are beyond our control, recommendations are made without warranty or guarantee.