STRONGBOND ONE SHOT - 303

| SB-OS is a water soluble Aminoplastic Synthetic Powder Resin based closed contact adhesive system. It gives exceptionally strong, hot water resistant infusible bond. SPECIFICATION SB-OS conforms to BS:1204: Part 2 (Type MR). | STRONBOND-ONE SHOT |
| --- | --- |

APPLICATION

Suitable for furniture assembly, edge gluing; cold setting adhesive for Cork Board, Plywood, Particle Board, MDF Board, Laminates; filling knots in cut wooden planks; assembling of block board buttoms; splicing of veneers.

PHYSICAL PROPERTIES

| Appearance | : | White Free Flowing Powder |  |
| --- | --- | --- | --- |
| Bulk Density | : | 0.75 + 0.05 gm/c.c. |  |
| Solubility | : | Soluble in cold water. |  |

POT LIFE TABLE

Pot Life Table-I (For SB-One Shot - A)

| Resin : Water | Temperature (Deg. C)B |  |  |
| --- | --- | --- | --- |
|  | 25 | 30 | 35 |
| 100 : 50 | 2 Hrs 45 Min. | 2 Hrs 00 Min. | 1 Hrs 30 Min. |
| 100 : 60 | 3 Hrs 00 Min. | 2 Hrs 15 Min. | 1 Hrs 45 Min. |

Pot Life Table-II (For SB-One Shot - B)

| Resin : Water | Temperature (Deg. C)B |  |  |
| --- | --- | --- | --- |
|  | 25 | 30 | 35 |
| 100 : 50 | 1 Hr 30 Min | 1 Hr 00Min. | 40 Min. |
| 100 : 60 | 2 Hrs 15 Min. | 1 Hr 30 Min. | 50 Min. |

Pot Life Table-III (For SB-One Shot - C)

| Resin : Water | Temperature (Deg. C)B |  |  |
| --- | --- | --- | --- |
|  | 25 | 30 | 35 |
| 100 : 50 | 1 Hr 20 Min. | 55 Min. | 35 Min. |
| 100 : 60 | 1 Hr 45 Min. | 1 Hr 15 Min. | 45 Min. |

PRESSING / CLAMPING TIME

Table For Clamping Time For SB-OS

| SB-OS | Glue Line Temperature (Deg. C)B |  |  |
| --- | --- | --- | --- |
|  | 25 | 30 | 35 |
| A | 3 Hrs | 2 Hrs 30 Min | 2 Hrs |
| B | 2 Hrs 35 Min. | 2 Hrs | 1 Hr 30 Min |
| C | 2 Hrs | 1 Hr 30 Min. | 1 Hr |

INSTRUCTION FOR USE

Typical Mixing Ratio

| SB-OS | : | 2 parts by weight |  |
| --- | --- | --- | --- |
| Water | : | 1 part by weight |  |

: 
:

MIXING PROCEDURE

Use a clean dry container and add water to the powder gradually, stirring continuously to ensure the powder is properly dispersed until the solution is free from lumps. This mixed adhesive is now ready for use.

SURFACE PREPARATION OF MATERIAL TO BE BONDED

Ensure that the surfaces to be bonded are smooth, clean uniformly thick and free from dust or other deposits. Surfaces should be thoroughly sanded before gluing along the grains of the timber. All surfaces must be wiped clean after sanding and left in a clean condition.

MOISTURE CONTENT

Moisture content of the surfaces at the time of gluing should be 10-14 %.

SPREAD RATE

Spread should be in the range of 200 - 400 gms/ Sq M.

METHOD OF APPLICATION

Apply the adhesive mix thinly and uniformly to one surface using either a brush, wooden rod, or hand roller, then assemble the joint and apply full clamping pressure and good contact.

ASSEMBLY TIME ( PRESSING TIME)

After applying the adhesive, joints should be assembled, whilst the glue line is still moist. Good contact can be assured.

BONDING PRESSURE

Depending on type of surface to be bonded and equipment available good surface contact should be assured by giving adequate pressure.

CLEANING

Mixing and gluing equipment can be cleaned with warm water. Once the glue has hardened, it is insoluble and must be scrapped off.

STORAGE

The resin should be stored in original bags in a dry place and kept as cool as possible.

SHELF LIFE

6 months at 30deg C and 65% RH.

PACKING

25 Kgs PP woven sacks with polyethylene inner liner.

NOTE

Information on this data sheet is based on the best of our knowledge. However, since conditions under which our products may be used are beyond our control, recommendations are made without warranty or guarantee.