# SB – OS 503S

Introduction:  SB-OS 503S is a self-catalyzed Amino-Plastic Powder generally used for tape less veneer splicing of any thickness.  The glue made out of it is cream colour.

Physical Properties:

## Form			:	Dry Free Flowing Powder

Colour			:	Cream

#### Shelf Life		:	6 months at 30 deg.C

Pot Life		:	4 hours at 32 deg.C.

Mixing Formulations:

SB-OS 503S 		:	100 parts by weight.

Water			:	 60 parts by weight.

Viscosity at 32 deg.C	:	1200-1500 cps.

Mixing Procedures:

Add powder to water and mix it thoroughly until a homogeneous mixture is obtained.  Pot Life can be adjusted in high atmospheric temperature by adding liq. Ammonia to the mix.

Storage:  Material should be kept in a cool and dry place inside a tightly closed container.

NoteNote:  Information on this publication is based on the best of our knowledge and experience. However, since conditions under which our products may be used are beyond our control, recommendations are made without warranty or guarantee.