#### SAWN WOOD SPECIFICATIONS – CEDRO ROSA, BRAZIL

CedroRosa
COMMON NAME

Cedrela odorata

SCIENTIFIC NAME

Meliaceae

FAMILY

Jamari

ORIGIN

COMMON NAMES: Acaju,Capiúva,Cedreilro,Cedro-amargo,Cedro-amargoso,Cedro-aromático,Cedro-batata,Cedro-bordado,Cedro-branco,Cedro-bravo,Cedro-do-amazonas,Cedro-do-paraguai,Cedro-fêmea,Cedro-manso,Cedro-mogno,Cedro-verdadeiro,Cedro-vermelho

Drying

General Characteristics

Tree

Workability

PHYSICAL PROPERTIES

Density(g/cm3) 		Shrinkage (%) 	Shrinkage Tangential/ Shrinkage Radial

Dry Green Basic 	Aparente Tangential 	Radial Volumetric

0,49 1,06 0,39 0,47 	12,1 9,06 21 		1,3

MECHANICAL PROPERTIES

State Static Bending 			Compression 				Janka Hardness

Modulus of rupture (kgf/cm2) 	Modulus of elasticity (1.000kgf/cm2) Parallel to the grain Perpendicular to the grain 		Parallel to the grain (kgf) 		End to the grain (kgf)

Maximum compression (kgf/cm2) Stress at proportional limit (kgf/cm2)

Green 448 84 				229 23 				287 268

Dry 768 99 				535 46 				614 445

State Tension 			Cleavage strength Shear 			Nail extration

Perpendicular to the grain 	Maximum compression (kgf/cm) Maximum compression (kgf/cm) Parallel to the grain (kgf) End to the grain (kgf)

Maximum compression (kgf/cm2)

Green 30 40 			63 						36 62

Dry 29 41 			70 						58 72